### SPECIFICATIONS

# For

SHADE CLOTH

See SECTION 12494 – 2.3 SHADE CLOTH

### Choose desired fabric and insert into Division 12 Specifications

## LIGHT-FILTERING FABRICS

  - SheerWeave Infinity (3% open) by Phifer.  Openness Factor:  Approximately 3%.  Composition:  100% TPO (Thermoplastic Olefin), 30% TPO fiber yarn / 70% TPO coating on TPO yarn.  Breaking Strength (lb):  176 Warp, 153 Fill.  Fire Classification:  NFPA 701-2004 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22. GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate. Available Patterns and Colors:  PG1 Cotton, PG2 Almond, PG Wheat, PG4 Stone, QG1 Barley, VG1 Nickel, VG2 Midnight, VG3 Black, and VG4 Slate.

2	SheerWeave Infinity (5% open) by Phifer.  Openness Factor:  Approximately 5%.  Composition:  100% TPO (Thermoplastic Olefin), 30% TPO fiber yarn / 70% TPO coating on TPO yarn.  Breaking Strength (lb):  173 Warp, 130 Fill.  Fire Classification:  NFPA 701-2004 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate. Available Patterns and Colors:  PG1 Cotton, PG2 Almond, PG3 Wheat, PG4 Stone, QG1 Barley, VG1 Nickel, VG2 Midnight, VG3 Black, and VG4 Slate

3	SheerWeave Style 1000 (25%) by Phifer:  Openness Factor:  Approximately 25%.  Composition: 35% Fiberglass, 65% Vinyl on Fiberglass.  Breaking Strength (lb):  215 Warp, 95 Fill (PO2 White), 215 Warp, 105 Fill (PO3 Almond White). Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Std. 5867 2008, Part 2 Type B Performance and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM G21 and ASTM G22.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  PO2 White, and PO3 Almond White

4	SheerWeave Style 2000 (5%) by Phifer:  Openness Factor:  Approximately 5%.  Composition: 37% Fiberglass, 63% Vinyl on Fiberglass.  Breaking Strength (lb):  260 Warp, 270 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Std. 5867 and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  PO2 White, PO4 White/Bone, PO5 White/Platinum, QO5 Bone, QO6 Bone/Platinum, Q1O Bronze, VO4 Platinum, V21 Charcoal, V22 Charcoal/Gray, and V24 Charcoal/Chestnut.

5	SheerWeave Style 2100 (10%) by Phifer:  Openness Factor:  Approximately 10%.  Composition: 37% Fiberglass, 63% Vinyl on Fiberglass.  Breaking Strength (lb):  260 Warp, 200 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Std. 5867 and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate. Available Patterns and Colors:  PO2 White, PO4 White/Bone, PO5 White/Platinum, QO5 Bone, QO6 Bone/Platinum, Q1O Bronze, VO4 Platinum, V21 Charcoal, V22 Charcoal/Gray, and V24 Charcoal/Chestnut.

6	SheerWeave Style 2390 (5%) by Phifer:  Openness Factor:  Approximately 5%.  Composition: 35% Fiberglass, 65% Vinyl on Fiberglass.  Breaking Strength (lb):  250 Warp, 235 Fill.  Fire Classification:  M 1 (Style 2390), California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Std. 5867 2008, Part 2 Type B Performance, and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180, ASTM G22 AATCC90 Part 3, ASTM G21, ASTM D3273.  GREENGUARD Mold and Bacteria Standard ASTM 6329; includes Microban antimicrobial additives. Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P14 Oyster/Pearl Gray, Q20 Beige, Q21 Beige/Pearl Gray, V20 Pearl Gray, V21 Charcoal, V22 Charcoal/Gray, and V24 Charcoal/Chestnut.

7	SheerWeave Style 2360 (10%) by Phifer:  Openness Factor:  Approximately 10%.  Composition: 35% Fiberglass, 65% Vinyl on Fiberglass.  Breaking Strength (lb):  255 Warp, 180 Fill.  Fire Classification:  M 1 (Style 2390), California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASDTM E2180, ASTM G22 AATCC90 Part 3, ASTM G21, ASTM D3273.  GREENGUARD Mold and Bacteria Standard ASTM 6329; includes Microban antimicrobial additives. Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P14 Oyster/Pearl Gray, Q20 Beige, Q21 Beige/Pearl Gray, V20 Pearl Gray, V21 Charcoal, V22 Charcoal/Gray, and V24 Charcoal/Chestnut.

8	SheerWeave Style 2410 (3%) by Phifer:  Openness Factor:  Approximately 3%.  Composition: 35% Fiberglass, 65% Vinyl on Fiberglass.  Breaking Strength (lb):  255 Warp, 325 Fill.  Fire Classification:  M 1 (Style 2390), California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180, ASTM G22 AATCC90 Part 3, ASTM G21, ASTM D3273.  GREENGUARD Mold and Bacteria Standard ASTM 6329; includes Microban antimicrobial additives. Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P14 Oyster/Pearl Gray, Q20 Beige, Q21 Beige/Pearl Gray, V20 Pearl Gray, V21 Charcoal, V22 Charcoal/Gray, and V24 Charcoal/Chestnut.

9	SheerWeave Style 2500 (1%) by Phifer:  Openness Factor:  Approximately 1%.  Composition: 37% Fiberglass, 63% Vinyl on Fiberglass.  Breaking Strength (lb):  380 Warp, 338 Fill.  Fire Classification:  M 1 (Style 2390), California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180, ASTM G22 AATCC90 Part 3, ASTM G21, ASTM D3273.  GREENGUARD Mold and Bacteria Standard ASTM 6329; includes Microban antimicrobial additives. Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P14 Oyster/Pearl Gray, Q20 Beige, Q21 Beige/Pearl Gray, V20 Pearl Gray, V21 Charcoal, V22 Charcoal/Gray, and V24 Charcoal/Chestnut.

10	SheerWeave Style 2701 (1%) by Phifer:  Openness Factor:  Approximately 1%.  Composition: 36% Fiberglass, 64% Vinyl on Fiberglass.  Breaking Strength (lb):  264 Warp, 377 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180.  GREENGUARD Children & School certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P28 Oyster/Charcoal, and P91 Oyster/Pewter, and P92 Oyster/Chestnut.

11	SheerWeave Style 2703 (3%) by Phifer:  Openness Factor:  Approximately 3%.  Composition: 36% Fiberglass, 64% Vinyl on Fiberglass.  Breaking Strength (lb):  247 Warp, 312 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard, 5867 and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P28 Oyster/Charcoal, and P91 Oyster/Pewter, and P92 Oyster/Chestnut.

12	SheerWeave Style 2705 (5%) by Phifer:  Openness Factor:  Approximately 5%.  Composition: 34% Fiberglass, 66% Vinyl on Fiberglass.  Breaking Strength (lb):  279 Warp, 240 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Std. 5867 and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P28 Oyster/Charcoal, and P91 Oyster/Pewter, and P92 Oyster/Chestnut.

13	SheerWeave Style 2710 (10%) by Phifer:  Openness Factor:  Approximately 10%.  Composition: 34% Fiberglass, 66% Vinyl on Fiberglass.  Breaking Strength (lb):  283 Warp, 220 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard, 5867 and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P12 Oyster, P13 Oyster/Beige, P28 Oyster/Charcoal, and P91 Oyster/Pewter, and P92 Oyster/Chestnut.

14	SheerWeave Style 3000 (14%) by Phifer:  Openness Factor:  Approximately 14%.  Composition: 35% Fiberglass, 65% Vinyl on Fiberglass.  Breaking Strength (lb):  250 Warp, 262 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), and NFPA 701 TM#2 (large scale).  Bacteria and Fungal Resistance:  ASTM E2180.  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P00 Spanish Gray, P01 Pearl White, Q01 Mushroom Sand, Q02 Custard Cream, Q04 Chocolate, Q17 Sand Dollar, Q18 Espresso, Q19 Honey Sage, V00 Dusty Grey, V01 Pale Grey, V02 Ninja Grey, V18 Mossy Green, and V19 Harvest Wheat.

15	SheerWeave Style 4000 (5%) by Phifer:  Openness Factor:  Approximately 5%.  Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  315 Warp, 260 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#2 (large scale) and CAN/ULC S 109-M-87.  Bacteria and Fungal Resistance:  ASDTM E2180 and ASTM G22  GREENGUARD Children & School certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P06 Chalk, P07 Alabaster, P10 Granite, Q12 Pebblestone, Q15 Greystone, Q16 Tobacco, V07 Pewter, V10 Ebony, and V15 Ash.

16	SheerWeave Style 4100 (10%) by Phifer:  Openness Factor:  Approximately 10%.  Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  315 Warp, 230 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#2 (large scale) and CAN/ULC S 109-M-87.  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P06 Chalk, P07 Alabaster, P10 Granite, Q12 Pebblestone, Q15 Greystone, Q16 Tobacco, V07 Pewter, V10 Ebony, and V15 Ash.

17	SheerWeave Style 4400 (3%) by Phifer:  Openness Factor:  Approximately 3%.  Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  340 Warp, 250 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#2 (large scale) and CAN/ULC S 109-M-87.  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P06 Chalk, P07 Alabaster, P10 Granite, Q12 Pebblestone, Q15 Greystone, Q16 Tobacco, V07 Pewter, V10 Ebony, and V15 Ash.

18	SheerWeave Style 4500 (5%) by Phifer:  Openness Factor:  Approximately 5%.  Composition: 17% Polyester, 83% Vinyl on Polyester.  Breaking Strength (lb):  181 Warp, 168 Fill.  Fire Classification:  California U.S. Title 19 (small scale), ASTM E 84 (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P06 Chalk, P10 Granite, Q59 Ecru, Q60 Golden Sand, U32 Linen, V07 Pewter, V10 Ebony, V44 Sandstone, V95 Cappuccino, and V96 Dark Bronze.

19	SheerWeave Style 4550 (5%) by Phifer:  Openness Factor:  Approximately 5%.  Composition: 17% Polyester, 83% Vinyl on Polyester.  Breaking Strength (lb):  182 Warp, 129 Fill.  Fire Classification:  California U.S. Title 19 (small scale) ASTM E 84, (Class 1), British Standard 5867 2008, Part 2 Type B Performance, and NFPA 701 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM G21 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P10 Granite, P65 Lenin, V45 Coal, and V47 Chestnut.

20	SheerWeave Style 4600 (3%) by Phifer:  Openness Factor:  Approximately 3%.  Composition: 22% Polyester, 78% Vinyl on Polyester.  Breaking Strength (lb):  183 Warp, 308 Fill.  Fire Classification:  California U.S. Title 19 (small scale), ASTM E 84 (Class 1), British Standard 5867 2008 Part 2 Type B Performance, and NFPA 701 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P06 Chalk, P10 Granite, Q59 Ecru, Q60 Golden Sand, U32 Linen, V07 Pewter, V10 Ebony, V44 Sandstone, V95 Cappuccino, and V96 Dark Bronze

21	SheerWeave Style 4650 (3%) by Phifer:  Openness Factor:  Approximately 3%.  Composition: 17% Polyester, 83% Vinyl on Polyester.  Breaking Strength (lb):  180 Warp, 135 Fill.  Fire Classification:  California U.S. Title 19 (small scale) ASTM E 84, (Class 1), British Standard 5867 2008, Part 2 Type B Performance, and NFPA 701 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM G21 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P10 Granite, P65 Lenin, V45 Coal, and V47 Chestnut.

22	SheerWeave Style 4700 (5%) by Phifer:  Openness Factor:  Approximately 5%.  Composition: 21% Polyester, 79% Vinyl on Polyester.  Breaking Strength (lb):  190 Warp, 285 Fill.  Fire Classification:  NFPA 701 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  T90 Quartz, T91 Champagne, T92 Chrome, T93 Antique Gold, T94 Russet, T95 Silver Smoke, and T96 Black Pearl.

23	SheerWeave Style 4800 (1%) by Phifer:  Openness Factor:  Approximately 1%.  Composition: 24% Polyester, 76% Vinyl on Polyester.  Breaking Strength (lb):  400 Warp, 120 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), NFPA 101 (Class A Rating), UBC (Class 1), British Standard 5867 2008 Part 2 Type B Performance, NFPA 701 TM#2 (large scale) and CAN / ULC S 109-M-87.  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P06 Chalk, P07 Alabaster, P75 Pearl, Q97 Sand, Q98 Mocha, Q99 Taupe, V10 Ebony, V16 Grey, V59 Fleece, V60 Clay, V61 Mink, and V62 Flint.

.

- SheerWeave Style 5000 Natural by Phifer:

  - P60 Bamboo/Birch (10%), Openness Factor: Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  330 Wrap, 180 Fill.  Fire Classification: California U.S. Title 19, (small scale), NFPA-701-2004 TM #1 (small and large scale), British Standard 5867, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q43 Marble/Sand (5%). Openness Factor:  Approximately 5%. Composition: 28% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  330 Wrap, 180 Fill.  Fire Classification: California U.S. Title 19, (small scale), NFPA-701-2004 TM #1 (small and large scale), British Standard 5867, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - P46 Bamboo/Wheat (7%). Openness Factor:  Approximately 7%. Composition: 27.5% Polyester, 67% Vinyl on Polyester, 5.5% Acrylic.  Breaking Strength (lb):  330 Wrap, 200 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q47 Moire/Mocha (7%). Openness Factor:  Approximately 7%. Composition: 26.3% Polyester, 67.7% Vinyl on Polyester, 6% Acrylic.  Breaking Strength (lb):  330 Wrap, 100 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q48 Bark/Cedar (10%). Openness Factor:  Approximately 10%. Composition: 26.3% Polyester, 67.7% Vinyl on Polyester, 6% Acrylic.  Breaking Strength (lb):  330 Wrap, 100 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q49 Rattan/Umber (7%). Openness Factor:  Approximately 7%. Composition: 27.5% Polyester, 67% Vinyl on Polyester, 5.5% Acrylic.  Breaking Strength (lb):  330 Wrap, 200 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q50 Bark/Tiger Oak (7%). Openness Factor:  Approximately 7%. Composition: 27.5% Polyester, 67% Vinyl on Polyester, 5.5% Acrylic.  Breaking Strength (lb):  330 Wrap, 200 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q51 Wicker/Mushroom (5%). Openness Factor:  Approximately 5%. Composition: 27.5% Polyester, 67% Vinyl on Polyester, 5.5% Acrylic.  Breaking Strength (lb):  330 Wrap, 200 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q53 Honeycomb/Brown Sugar (10%). Openness Factor:  Approximately 10%.  Composition: 26.3% Polyester, 67.7% Vinyl on Polyester, 6% Acrylic.  Breaking Strength (lb):  345 Wrap, 145 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q94 Tweed/Oatmeal (5%). Openness Factor:  Approximately 5%. Composition: 23% Polyester, 64% Vinyl on Polyester, 13% Uncoated Polyester.  Breaking Strength (lb):  352 Wrap, 136 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q95 Tweed/Buckeyel (5%). Openness Factor:  Approximately 5%. Composition: 23% Polyester, 63% Vinyl on Polyester, 14% Uncoated Polyester,  Breaking Strength (lb):  341 Wrap, 124 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - Q96 Thatch/Wheatgrass (7%). Openness Factor: Approximately 7%.  Composition: 27% Polyester, 68% Vinyl on Polyester, 5% Olefin.  Breaking Strength (lb):  339 Wrap, 153 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - R11 Linen/Cranberry (3%). Openness Factor:  Approximately 3%. Composition: 45% Polyester, 55% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 125 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - R12 Linen/Cinnamon (3%). Openness Factor:  Approximately 3%. Composition: 45% Polyester, 55% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 125 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U10 Linen/Topaz (3%). Openness Factor:  Approximately 3%. Composition: 45% Polyester, 55% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 125 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U11 Linen/Burlap (3%). Openness Factor:  Approximately 3%. Composition: 43% Polyester, 57% Vinyl on Polyester. Breaking Strength (lb):  320 Wrap, 263 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U12 Linen/Cream (3%). Openness Factor:  Approximately 3%. Composition: 43% Polyester, 57% Vinyl on Polyester. Breaking Strength (lb):  320 Wrap, 263 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U13 Crepe/Jade (10%). Openness Factor:  Approximately10%. Composition: 28% Polyester, 72% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U14 Crepe/Walnut (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U15 Crepe/Granola (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U16 Crepe/Toasted Coconut (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - V88 Linen/Fig (3%). Openness Factor:  Approximately 3%. Composition: 45% Polyester, 55% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 125 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - V89 Crepe/Blacken Bronze (10%). Openness Factor:  Approximately 10%. Composition: 27% Polyester, 73% Vinyl on Polyester. Breaking Strength (lb):  359 Wrap, 124 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - V90 Crepe/Chestnut (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester. Breaking Strength (lb):  341 Wrap, 125 Fill.  Fire Classification: California U.S. Title 117, Section E. Part 1, NFPA 101 (Class A Rating), and UBC (Class 1) Bacteria and Fungal Resistance:  ASTM E 2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

- SheerWeave Style 5000 Contemporary by Phifer:

  - U17 Digital Lines/Pear Black (10%). Openness Factor:  Approximately 10%. Composition: 27% Polyester, 73% Vinyl on Polyester.  Breaking Strength (lb):  359 Wrap, 124 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U17 Digital Lines/Crystal (10%). Openness Factor:  Approximately 10%. Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  334 Wrap, 80 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

  - U19 Digital Lines/Polished Silver (10%). Openness Factor:  Approximately 10%. Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  334 Wrap, 80 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.

D.  U20 Filigree/Frost (7%). Openness Factor:  Approximately 7%. Composition: 27%   Polyester, 73% Vinyl on Polyester.  Breaking Strength (lb):  359 Wrap, 124 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

E.	U21 Filigree/Polished Silver (7%). Openness Factor: Approximately 7%.  Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  334 Wrap, 80 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

F.	U22 Filigree/Light Copper (7%). Openness Factor:  Approximately 7%. Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  334 Wrap, 80 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

G.	U23 Filigree/Crystal (7%). Openness factor:  Approximately 7%. Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  334 Wrap, 80 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

H.	U24 Seaglass/Silver (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

I.	U25 Seaglass/Copper (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

J.	U26 Seaglass/Gold (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

K.	U27 Seaglass/Verde (10%). Openness Factor:  Approximately 10%. Composition: 27% Polyester, 73% Vinyl on Polyester.  Breaking Strength (lb):  359 Wrap, 124 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

L.	U28 Seaglass/Chardoney (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

- U29 Seaglass/Crystal (10%). Openness Factor:  Approximately 10%. Composition: 28% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  341 Wrap, 175 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

N.	U30 Digital Lines/Shimmer (10%). Openness Factor:  Approximately 10%. Composition: 25% Polyester, 72% Vinyl on Polyester.  Breaking Strength (lb):  334 Wrap, 80 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

O.	U31 Digital Lines/Caramel (10%). Openness Factor:  Approximately 10%. Composition: 25% Polyester, 75% Vinyl on Polyester.  Breaking Strength (lb):  334 Wrap, 80 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

P.	V91 Digital Lines/Raven (10%). Openness Factor:  Approximately 10%. Composition: 27% Polyester, 73% Vinyl on Polyester.  Breaking Strength (lb):  359 Wrap, 124 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

Q.	V92 Filigree/Toffee (7%). Openness Factor:  Approximately 7%. Composition: 27% Polyester, 73% Vinyl on Polyester.  Breaking Strength (lb):  359 Wrap, 124 Fill.  Fire Classification: California U.S. Title 117, Section E Part 1, NFPA 101 (Class A Rating), UBC (Class 1).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate

- SheerWeave Style 7000 (Blackout) by Phifer:  Openness Factor:  Opaque.  Composition: 100% Polyester with Acrylic Foamed Backing.  Breaking Strength (lb):  205 Warp, 225 Fill.  Fire Classification:  California U.S. Title 19 (small scale), NFPA 701-2004 TM #1 (small scale), British Standard 5867.  Bacteria and Fungal Resistance:  ASTM G21-96, AATCC 174 – 1998, Part II and III. GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  P62 White, P63 Birch, P64 Sand, Q57 Wheat, V39 Graphite, V40 Onyx, V41 Canyon, and Q58 Mushroom.

26	SheerWeave Style 7100 (Blackout) by Phifer:  Openness Factor:  Opaque.  Composition:  Vinyl-coated fiberglass fabric laminated with two-ply 100% PVC blackout film. Breaking Strength (lb):  253 Warp, 263 Fill.  Fire Classification:  California U.S. Title 19 (small scale) NFPA 701-2004 TM#1 (small scale), British Standard 5867 2008 Part 2 Type B Performance.  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22. (Note Microban on face only)  GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Avail Patterns and Colors:  P02 White, P04 White/Bone, P05 White/Platinum, Q05 Bone, Q06 Bone/Platinum, and V21 Charcoal.

27	SheerWeave Style 7300 (Blackout) by Phifer:  Openness Factor:  Opaque.  Composition:  100% Polyester with Acrylic Foamed Backing (PVC Free). Breaking Strength (lb):  118 Warp, 136 Fill.  Fire Classification:  California U.S. Title 19 (small scale), NFPA 701 – 2004 TM #1 (small scale).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22. GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors: R23 Salt, R24 Shell, R25 Shore, R26 Glow, R27 Grove, R28 Cobble, R29 Hide, and R30 Ink.

28	SheerWeave Style 7350 (Light Filtering) by Phifer:  Openness Factor:  Light Filtering.  Composition:  100% PVC Polyester (PVC Free). Breaking Strength (lb):  134 Warp, 128 Fill.  Fire Classification:  California Technical Bullertin 117 E.  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22. GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors: R23 Salt, R24 Shell, R25 Shore, R26 Glow, R27 Grove, R28 Cobble, R29 Hide, and R30 Ink.

29	SheerWeave Style 7500 (Blackout) by Phifer:  Openness Factor:  Opaque.  Composition:  100% Polyester with Acrylic Coating (PVC Free). Breaking Strength (lb):  160 Warp, 167 Fill.  Fire Classification:  California U.S. Title 19 (small scale) and NFPA 701 – 2004 TM#1 (small scale).  Bacteria and Fungal Resistance:  ASTM E2180 and ASTM G22. GREENGUARD Children & School Certified as a low emitting fabric.  Manufacturer to supply GREENGUARD Children & School Certificate.  Available Patterns and Colors:  R13 Ice, R14 Coconut, R15 Loft, R16 Spirit, R17 Dune, R18 Starfish, R19 Stone, R20 Odyssey, R21 Orient, and R22 Midnight.

END OF SECTION